## Slide 1: Simulation of thin film growth
Shawn Wimer
4/26/2024

## Slide 2: Contents
Brief overview of thin film growth
Growth equations
Molecular dynamics
Ballistic deposition
Monte Carlo method

## Slide 3: Thin film growth

## Slide 4: Thin film deposition
Material flux directed at substrate
  Physical vapor deposition, sputtering, chemical vapor deposition, etc.
Particles can have any trajectory but the distribution depends on method and system setup
Particles can adhere become part of a film that grows on the surface or be reemitted
Thin film growth

## Slide 5: Early stage of film growth
Island formation or layer-by-layer growth depends on surface energies
  Frank-van der Merwe (layer-by-layer):
  Volmer-Weber (islands):
  Stranski-Krastanov (intermediate): Film begins layer-by-layer but transitions to island growth
Thin film growth
a) FM, b) VW, c) SK
Andersson 1982 [1]

## Slide 6: Coalescence in island growth
Islands are isolated until they grow into each other and begin coalescence
Eventually a network of connected islands and isolated voids forms
  “Percolated”
Further deposition fills the voids
The time to coalescence is increased by more diffusion and decreased by higher deposition rate
Thin film growth
Copper on a-carbon deposition over time
Colin 2020 [2]

## Slide 7: Growth equations

## Slide 8: Thin film growth models
Very general descriptions of the interface with the volume above the surface
Simple model: the surface grows at a constant rate perpendicular to the surface at all points
Surface roughness increases until islands coalescence, then decreases
Growth equations

## Slide 9: Growth equations
Generally of the form
No specific form for general growth equation G; depends on symmetries in the growth behavior
  Time, position, rotational symmetries…
Note that h is single-valued
is a noise term
Growth equations
Single-valued
Not single-valued

## Slide 10: Noise term:
The noise term, , has some conditions:
The second condition implies that the noise should be uncorrelated in space and time
Two useful distributions:
  “Bounded choice” (choose -1 or 1)
  Normal/Gaussian
Growth equations

## Slide 11: Determine G
G is normally a differential equation, possibly non-linear
Hard way: solve for it knowing growth behavior
Easier way: reason towards it from symmetries in the growth
  Some differential terms and terms in t can be excluded
  , , , …
Possible symmetries:
  Time invariance
  Translation invariance in growth direction
  Rotation invariance about the growth direction
  Translation invariance in x
  Invariance about mean height ()
Growth equations

## Slide 12: Edwards-Wilkinson equation
If all symmetries can be applied the EW equation is found:
  is the ‘surface tension’ smoothing the surface
The mass of the interface doesn’t change
Growth equations

## Slide 13: Kardar-Parisi-Zhang equation
Reject one symmetry () to get the KPZ equation:
  is a nonlinear parameter that makes analytical solutions untenable
This equation changes the mass of the interface, driven by
Growth equations

## Slide 14: Limitations of growth equations
Many different growth models have been studied
  KPZ is a well-studied “universality class”
Often no analytical solutions
Use numerical techniques, but:
  Depends on space and time step sizes
  Much harder when spatial correlations play a heavy role
No information on the lattice or individual particles
Normally: simulate another way and compare to equations
Growth equations

## Slide 15
Let’s try simulating the process rather than the model
Growth equations

## Slide 16: Molecular dynamics
Enrico Fermi
(DOE)

## Slide 17: Molecular dynamics
Simulate the behavior of particles by implementing physical laws
Simulate how particles move according to the forces between them
Increasingly used in biology
  Protein shapes and interactions
Molecular dynamics
Knordlun on Wikipedia

## Slide 18: Using potentials
Create ‘force fields’ to model the forces between molecules
Apply them by Newtonian mechanics
  Can use quantum mechanics
Many possible potentials, including from theory or from experiment
  Choice depends on application
Molecular dynamics

## Slide 19: Potentials and forces
Molecular dynamics
Can use many intermolecular potentials but Lennard-Jones is very common:
Good for fast calculations as the two interior terms are relatable
Not rigorous but still explanatory

## Slide 20: Pros and cons
Bad computational scaling with increasing particles
Multi-body effects
Dependence on time step
Very short time scales
Answer: increase your computational resources or simplify the processes (or both)
  More computational power:
    Expensive
    Power scales slower than the problem
  Simplification:
    Less realistic
    Less intuitive
Molecular dynamics

## Slide 21
Let’s try abstracting the process
Molecular dynamics

## Slide 22: Ballistic deposition

## Slide 23: Ballistic deposition
Model individual particles as objects that collide with a surface
Developed to simulate sedimentation and aggregation in solution in 1950s/1960s
Later applied to vapor deposition simulations
Often described by KPZ equation
Ballistic deposition
Hard objects physically collide with each other and their confines

## Slide 24: Film features
Very porous and low-density
Rough with high surface area
Substrate tilt leads to individual structures similar to each other and self-similar (‘fractal-like’)
Ballistic deposition

## Slide 25: Simple ballistic deposition model
Create a 2D simulation area with a substrate along the bottom
Drop spheres one-by-one at random positions high above the substrate
Stick them where they land
Optionally, let each settle/relax/diffuse after it lands
Ballistic deposition

## Slide 26: On-lattice/off-lattice or discrete-/continuous-space
Simulations can take place in discrete- or continuous-space
  On-lattice and off-lattice, respectively
Discrete-space easier and faster but requires some assumptions
  Imposition of lattice
  Shape of particle
Most use discrete-space but early work was all continuous space
Ballistic deposition

## Slide 27: Incorporating randomness
(Probably) universally assume uniform distribution of incoming particle position
Particles can be modeled with an angular distribution
  Be careful to use it correctly
Diffusion can be randomized
Use Monte Carlo method to simulate process
Ballistic deposition

## Slide 28: Monte Carlo method basics
Use repeated random sampling to collect aggregate results
Useful for determining numerically what is difficult analytically
Large numbers of sampling are generally better, so computers are useful
Monte Carlo method

## Slide 29: Conclusion
Growth equations
Good:
  Well-studied equations
Bad:
  No overhangs
  No exact solution
  Time-step dependence
Conclusion
Molecular dynamics
Good:
  Directly apply physics
  Tailorable to needs
  Many mature methods
Bad:
  Slow; scales poorly
  Time-step dependence
Growth equations
Good:
  Fast
  Easily created
  Simple
Bad:
  Same problems as MD or discretized
  Time is arbitrary

## Slide 30: Bibliography
Andersson, “The Initial Growth of Vapour Deposited Gold Films”, Gold. Bull. 15 (1982)
Colin et al., “In Situ and Real-Time Nanoscale Monitoring of Ultra-Thin Metal Film Growth Using Optical and Electrical Diagnostic Tools”, Nanomaterials (2020)
Marjorie Vold, “Computer simulation of floc formation in a colloidal suspension”, Journal of Colloid Science 18, 684-695 (1963)
Barabasi and Stanley, “Fractal Concepts In Surface Growth”, Cambridge University Press (1995)
Bibliography

## Slide 31: Scaling exponent
Interface width :
  RMS fluctuation in surface height
  Saturates as correlation length approaches system size
Scaling exponent(s):
Different classes have different scaling exponents
Growth equations
Barabasi and Stanley, 1995 [4]

## Slide 32: Monte Carlo method
Stansilaw Ulam (Los Alamos National Laboratory)

## Slide 33: Monte Carlo method basics
Use repeated random sampling to collect aggregate results
Useful for determining numerically what is difficult analytically
Large numbers of sampling are generally better, so computers are useful
Procedure:
Determine the range of potential inputs
Draw samples from the range of inputs
Process the samples according to the model being analyzed
Record the individual and/or aggregate results
Monte Carlo method

## Slide 34: Monte Carlo considerations
Correctly sample the correct distribution!
Some advanced techniques exist to sample more complicated distributions
Increasingly used wherever statistics are useful
  Particle physics, finance, operations, etc.
Monte Carlo method

## Slide 35: Counter example: Sum of dice
Find chance of the sum of two dice to be 10 (independent dice)
Easy:
  Two uniform random variables, D1 and D2, in [1,6]
Easily extended to find the chance of any possible sum
  Just count the individual probabilities and sum them
Monte Carlo method not necessary here
Monte Carlo method

## Slide 36: Example: Complicated sum of dice
Roll four dice, reroll any 1s on the first throw, then sum the three largest:
  [4, 4, 1, 1] -> [4, 4, 2, 1] -> 10
Much more complicated to figure out analytically
Monte Carlo method

## Slide 37: Example: Complicated sum of dice
The quality of the results depends on the number of samples
More complicated processes might require many more samples, particularly to find the ends of the range
Monte Carlo method

## Slide 38
Examples